[image: image1]TSIRCON CO LTD
MANUFACTURERS & TRADERS

OF BUILDING MATERIALS


Ημ. έκδοσης 7/2006

Δ Joint Profile

Crack Inducer

[image: image3.png]



Description: An easily applied preformed PVC profile that induces controlled cracking in continuously laid concrete or screed. 

Advantages:

· Enables increased production. The concrete can be laid in the whole area in the same day.

· No need for costly cutting and filling of joints. 

· Very good anchoring in the concrete.

· Retains unchanged its shape and dimension. It can also be used as guidance for the leveling of concrete or screed.

· It can also be used in concrete floors subject to traffic loads.

Technical Characteristics:

	Material
	: Polyvinyl chloride compound, hard

	Density
	: 1,40g/ml

	Yield Strength
	: 46N/mm²
	(BS2782:Part II:Method 1110)

	% of Elongation
	: 40% 
	

	Modulus of Elasticity
	: 2000N/mm²

	Vicat Softening Temperature
	: 82°C
	(BS2782:Part I:Method 120B)








PAGE  
	Head office: 

Strovolos Industrial Zone,

P.O. Box 23863, 1687 Nicosia, CYPRUS.

Tel: +357 22 - 487029, Fax: +357 22 - 487716

htpp://www.tsircon.com



[image: image2.png]


