[image: image1.png]


TSIRCON CO LTD
MANUFACTURERS & TRADERS

OF BUILDING MATERIALS


GARDTEX II

JOINT SEALANT

1. PRODUCT NAME

GARDTEX II is one-part, moisture cured, self-leveling or gun grade, non-staining, polyurethane sealant which cures at ambient temperature to a firm, flexible tear-resistant rubber. It is highly resilient and has excellent recovery characteristics after extended periods of compression or elongation. 

2. MANUFACTURER

Tsircon Co. Ltd., P.O. Box 23863, 

1687 Nicosia, Cyprus, 

Tel: 02-487029, Fax: 02-487716

Under license by:

Texmastic International Inc., 

P.O. Box 210309, Dallas, 

Texas 75211-0309,

Tel:(214)330-4605, Fax:(214)331-5575

3. PRODUCT DESCRIPTION

Composition: Polyurethane based joint sealant.

Basic Uses: For sealing and caulking all joints that are subject to contraction and expansion. Bonds to concrete, wood, glass and metal.

Limitation: Containers that have been opened must be used within one or two days since it is moisture reactive material it sets up when exposed to air. All surfaces must be completely free of foreign matter. No primer is needed when the substrate is non-porous and clean. However if the substrate is porous, like mortar or concrete, then Sealant Primer 1 is recommended. 

Color: Grey and white are the standard colors. For big quantities other colors can be produced upon request.

Pack size: 

Gardtex II-A in sausages of 500cc

Gardtex II-B in sausages of 600c

Standards:  Federal Specification TT-S-230 and ANSI Specification A116.1-1967.

4. TECHNICAL DATA

GARDTEX II-A is pourable

GARDTEX II-B is gun-grade

Tack Free Time
: 24 hrs at 20°C and 50% R.H.

Cure Time
: 10 days at 20°C and 50% R.H.

Hardness
: 35 Shore A ± 5 after 14 days at room temperature

Elongation 
: >600%

At break

Tear Resistance
: 2,0 N/mm² 

(DIN 53504)

100% Modulus
: 0,7N/mm²

(appr. DIN 53504)

Above data are typical properties, individual batches may vary to a minor degree.

5. INSTALLATION

Joint Design: Suitable for all properly designed joints following accepted engineering practices. Joint width must be a minimum of 4 times the anticipated movement.

Surface Preparation: All joints must be absolutely clean. All curing compounds, old caulks, grease, waterproofing compounds, etc., must be removed. For non-porous surfaces such as glass, metal, etc., cleaning with MEK or Toluene is recommended. For porous substrates, Sealant Primer 1 is recommended to be used prior to the application of the sealant. In such a case, the primer must be left to dry and the sealant is applied before any dirt is picked up again. Polyethylene rod or polyurethane foam is recommended as a joint-filler and back-up material. In case there is bituminous impregnated filler, this must be separated from the sealant by Vinyl Tape or polyethylene film.

Application: 

Gardtex II-A is pouring grade and it is supplied in sausages. Either apply directly from sausage or by using a barrel gun (hand-operator application gun).

Gardtex II-B is gun-grade and it is supplied in sausages. Either apply by the use of a putty knife directly from the sausage or by the use of barrel gun.

6. PRODUCT WARRANTY

All products proven to be defective in manufacture will be replaced at no charge. Since the use of these products is beyond our control we cannot assume any risk or liability for results obtained, nor can we accept damages in excess of the purchase price of these products.

7. MAINTENANCE

If GARDTEX II is damaged and the joint has not been contaminated, it can be repaired by cutting out that part and resealing it with GARDTEX II.
	Head office: 

Strovolos Industrial Zone,

P.O. Box 23863, 1687 Nicosia, CYPRUS.

Tel: +357 22 48 70 29 , Fax: +357 2-487716

htpp://ww.tsircon.com



