[image: image2.emf] 

TSIRCON CO LTD
MANUFACTURERS & TRADERS

OF BUILDING MATERIALS


Ημ. έκδοσης 8/2010
TSIRCO-FLOPROOF 1

Normal setting integral waterproofer

An effective dispersed waterproofing admixture suitable for all kinds of cement mixes

Product: Integral water-repellent admixture and permeability eliminator for mass and reinforced concrete, renders and screeds.

Composition: Complex blend of inorganic silicates carried in an inert gelatinous dispersing agent.

Purpose: To prevent water absorption by cement-bound mixes and to eliminate their permeability.

Usage: 5-6 litres TSIRCO-FLOPROOF 1 are required to dose 1 cubic meter of concrete. For screeds and renders, TSIRCO-FLOPROOF 1 should constitute a part equal to 10% of the volume of the gauging water.

Pack: 4,20 and 210 litres.

Watertight Structures: The concrete is waterproofed throughout its entire mass.

Increased Durability: Improved resistance to chemical attack. Better protection of reinforcing steel. Increased resistance to frost. No reduction of concrete strength.

Better Appearance: TSIRCO-FLOPROOF 1 maintains the clean appearance of concrete and renders for longer periods. It also reduces efflorescence.

Introduction: All concrete structures can be penetrated by water not only though the joints, but also through the pores, created in the concrete by the evaporation of excess water not taken up by the hydration of cement. The penetrating water may cause corrosion of the steel reinforcement leading to spalling, or in the case of mass concrete, renders and screeds, it may cause serious damage by alternative freezing and thawing. The penetrating water may also carry deleterious substances or atmospheric impurities, which will cause damage in depth to the structure due to chemical attack. TSIRCO-FLOPROOF 1 is specially formulated to protect concrete structures against such deterioration, by reducing or eliminating the permeability of concrete and by making it water repellent. TSIRCO-FLOPROOF 1 has been demonstrated by independent tests. Thousands of waterproofing contracts have been carried out successfully both in Cyprus and overseas.

Properties: TSIRCO-FLOPROOF 1 is a complex blend of materials incorporating inorganic silicates carried in an inert gelatinous dispersing agent. Supplied in the form of a yellow liquid, the product must be diluted with water before it is used. Added to concrete or mortar, TSIRCO-FLOPROOF 1 causes an insoluble water-repellent lining which is formed around the pores of the entire mix. It also causes insoluble crystals which are formed in the pores themselves, in this way it reduces the permeability of the hardened mix. TSIRCO-FLOPROOF 1 is carefully formulated to protect the mix from excessive air entrainment thus the strength of the concrete is kept unaffected. TSIRCO-FLOPROOF 1 does not affect the setting time of concrete or mortar.

TSIRCO-FLOPROOF 1 is highly recommended as a waterproofing admixture for exterior concrete and renderings. It’s excellent water-repelling qualities will prevent dirt and other atmospheric impurities from penetrating into the structure. As they are washed off by rain, the clean natural appearance of the building will stay unaffected for longer periods. TSIRCO-FLOPROOF 1 will also increase the resistance of Ordinary Portland Cement against attack by oils, thus extending the life of screeds and renders which are liable to be attacked by oily or other chemical substances. TSIRCO-FLOPROOF 1 is suitable for use with ordinary or rapid hardening Portland cement and with sulphate-resisting cement. TSIRCO-FLOPROOF 1 may be used in conjunction with any of the other integral admixtures manufactured by TSIRCON CO LTD.

Where to use: TSIRCO-FLOPROOF 1 will have an excellent and long-lasting waterproofing effect on mass and reinforced concrete, sand /cement screeds and renders, precast concrete units, artificial stone and granolithic pavings. The product has been extensively used for waterproofing concrete structures which come frequently in contact with water. It is highly recommended for waterproofing basements, foundations, floors, ducts, retaining walls, swimming pools, storage tanks, boiler houses, grain drying pits etc.
How to use:
1. To obtain waterproof concrete 

Add a dose of 5-6 litres of TSIRCO-FLOPROOF 1 for every cubic meter of concrete. Before adding it into the concrete dilute TSIRCO-FLOPROOF 1 with an equal volume of water. When calculating the amount of water into the mix the amount of TSIRCO-FLOPROOF 1 must be included.

2. To obtain waterproofing screeds and renders 

Apply a dose of 1 part TSIRCO-FLOPROOF 1 to 10 parts of mixing water. At this ratio 4,5-5 litres of TSIRCO-FLOPROOF 1 will be sufficient for the following:

	Thickness of screed or render
	3:1 sand/cement mix
	2 ½: 1 grano mix

	12mm
20 mm

25mm
	22m²

15,5 m²
 11 m²
	19m²
 13 m²
   9,5 m²


The figures provided in the table above should be used for guidance only. The actual quantities of TSIRCO-FLOPROOF 1 required for any particular mix will depend on the cement and water contents of the mix. TSIRCO-FLOPROOF 1 must be thoroughly dissolved in the mixing water before incorporating into the mix. Diluted TSIRCO-FLOPROOF 1 which is to be used in subsequent batches must be stirred well so that the waterproofing is evenly distributed.

[image: image3.png]




[image: image1]
Important note: Never add concentrated TSIRCO-FLOPROOF 1 in the concrete mix. Always pre-dilute with water.

3. Treatment of joints
Careful attention must be paid to the joints of any water retaining structure especially if the structure is subject to movement. All joints must be formed in strict accordance to the Engineer’s design and instructions. Before adding the 

fresh concrete, the face of the joints must be hacked or scrubbed with a wire brush until the aggregate is exposed. The exposed surface must then be watered well and treated with a grout made of one part sand and one part cement mixed with TSIRCO-FLOPROOF 1 diluted with water in the ratio 1:10. Then the fresh mix can be poured.

4. Structures liable to water seepage

When applying screeds or renders to structures through which water is seeping under pressure, it is absolutely necessary to stop infiltration first. This can be achieved by lowering the water table or by using TSIRCO-FLOFAST CF.
Storage Life: Not less than one year provided the product is kept in manufacturers sealed containers and kept in frost-free conditions and away from direct sunlight. If the product becomes frozen it must be thawed out completely and stirred well before use.

How to Specify: Concrete/screed/render* shall be waterproofed with TSIRCO-FLOPROOF 1 used strictly in accordance with the instructions of the manufacturers TSIRCON CO LTD.

*Delete as applicable.

Note: For structures already exhibiting high water leakage under pressure, the successful waterproofing of the entire area is a highly skilled job. In such cases we recommend that the job is assigned to a specialist contractor who is well experienced in waterproofing systems. Our company is willing to offer advice on request.

Test results: The table below shows the effect of TSIRCO-FLOPROOF 1 on the permeability of concrete. Two identical mixes were prepared employing identical 1:2:4 mix proportions. One mix has dosed with TSIRCO-FLOPROOF1 and the other was kept as a control mix.

	Pressure of water held for one hour
	Amount of water percolating through specemens-ml

	Meters head
	p.s.i
	KN/m
	Plain concrete
	TSIRCO-FLOPROOF 1

Concrete

	15
	20
	138
	Nil
	Nil
	Nil
	No water percolated through the specimens at any stage of the tests

	22.5
	30
	207
	Nil
	Nil
	Nil
	

	30
	40
	276
	Nil
	Nil
	Nil
	

	38
	50
	345
	4
	4
	5
	

	56
	75
	517
	9
	8
	9
	

	75
	100
	689
	18
	20
	20
	

	94
	125
	861
	29
	33
	32
	

	113
	150
	1034
	42
	45
	51
	


�


1328-CPD-0001


TSIRCON CO LTD,  


Manufacturers of Building Materials


Βιομηχανική περιοχή Στροβόλου, 


Τ. K. 23863,1687 Λευκωσία, Κύπρος


06


1328-CPD-0042


ΕΝ 934-2


Water resisting admixture for concrete


EN934-2: T9


Maximum chloride content : 1.33 by mass


Maximum alkali content : ≤ 2.7  by mass








PAGE  
4
Page

	Head office: 

Strovolos Industrial Zone,

P.O. Box 23863, 1687 Nicosia, CYPRUS.

Tel: +357 22 - 48 70 29 , Fax: +357 22 - 487716

htpp://www.tsircon.com



