[image: image1.png]


TSIRCON CO LTD
MANUFACTURERS & TRADERS

OF BUILDING MATERIALS


Ημ. έκδοσης 1/2004

TSIRCO-FORM 1

Mould release agent

Product: Release agent for formwork. Improves surface finish for concrete.

Composition: Liquid of clear amber colour incorporating a rust inhibitor.

Purpose: To provide a quick, positive release of formwork, reducing labour costs and damage to moulds and formwork. To give high quality finishes to concrete.

Usage: Ready for use. One litre will treat approximately 30-40 square meters of formwork and/or moulds.

Pack: 4, 20 and 210 litre drums.

Advantages: Can be used with all types of formwork to provide easy, positive release. Reduces labour costs and damages. Reduces blowholes, surface blemishes and staining. Easily applied in very fine sprays. Economic coverage rates. Increased productivity.

Introduction: TSIRCO-FORM 1 is a chemical release agent, specially designed to give easy release of formwork and high quality finishes to concrete surfaces. The product can be applied immediately prior to casting or left to dry for several days prior to the use of the formwork. Extensive experience with TSIRCO-FORM 1 has shown that even after a two-week exposure to weather, treated forms will give excellent results and no re-treatment would be required.

TSIRCO-FORM 1 will normally dry within 1-2 hours from application to provide a safe-walking surface on soffit shutters. Furthermore, the treated surface is not affected by rain.

Properties:

Appearance: Clear amber liquid

Specific Gravity: 0.84 at 20oC.

Flash point (Pensky Martin closed cup): 75oC.

Viscosity: 5.23 cP at 20oC.

Where to use: TSIRCO-FORM 1 is suitable for use with all types of formwork and moulds and is suitable to be used for both white and grey cements without staining.

How to use: TSIRCO-FORM 1 is free of sediments and is a highly mobile liquid. It is best applied by spray and will not clog fine jets even at very low temperatures. The product can also be applied by fine-hair brush, sponge or roller. However, for the most economical use a fine fog spray is recommended. During application, care must be taken to achieve an even layer over the entire surface area, and this should be as thin as possible. Any excess liquid should be mopped up. Casting can follow immediately after treatment or later, until the treated surface appears to be dry. Experience has shown TSIRCO-FORM 1 to give excellent results even when the treated forms have been exposed to weather for several days. When treating new timber a first coat should be applied as a sealer and then a second coat before casting.

Usage: One litre of TSIRCO-FORM 1 will treat approximately 30-40 square meters of formwork or moulds. Cold weather, rough forms and hand application will normally require higher rates.

Storage Life: TSIRCO-FORM 1 will have an indefinite storage life provided the product is kept in manufacturers sealed containers. No special storage temperatures are required and experience has shown that even at temperatures down to _5oC the ingredients will not separate. Since the product is flammable it should never be stored near electrical equipment or near any sources of possible ignition.

Handling Precautions: TSIRCO-FORM 1 does not contain any materials, which are seriously hazardous to health. However, some precautions should be taken during handling or application. Prolonged contact with the skin should be avoided to prevent irritation. Workers should wear plastic or rubber gloves and clean overalls which must be worn to avoid inhalation of vapour and since the product is combustible smoking must not be allowed during handling. Drums must be re-sealed after each use.

PAGE  
1
Page

	Head office: 

Strovolos Industrial Zone,

P.O. Box 23863, 1687 Nicosia, CYPRUS.

Tel: +357 22 - 487029 , Fax: +357 22 - 487716

htpp://www.tsircon.com



