[image: image1.png]


TSIRCON CO LTD
MANUFACTURERS & TRADERS

OF BUILDING MATERIALS


Ημ. έκδοσης 1/2004

TSIRCO-POLY 107S

Special plaster for Squash Courts and other purposes

Product: A polymeric cement based finishing coat for direct application to fair-faced concrete, rendered brickwork or blockwork, and most cementitious surfaces.

Purpose: To provide a completely smooth finishing court system of uniform quality and appearance.

Packaging: 25kg three-ply paper sacks.

Advantages:

· A strong completely smooth finish, which does not necessarily require painting.

· A shrink-free, stress-eliminating system which avoids cracking associated with curing.

· Unique anti-condensation properties.
· Adequate working life (2hrs) in the hottest conditions.

· Simple and speedy application.

· Excellent bond to a wide range of building materials.

· Can be used as a repair system with minimum court close down.

Introduction: TSIRCO-POLY 107S is not a conventional wall plaster, but a retarded polymeric plaster specifically developed for the finishing of squash court walls with a fine 3mm layer. The material may be either applied monolithically on a polymer modified fibre-reinforced levelling base screed, or applied directly to a good quality fair-faced concrete wall.

Properties:

Colour: White, Grey, others upon request

Density: ≈ 2kg/lt

Pot Life: 45 minutes at 20oC

Compressive Strength (28 days at 20oC): 34-40N/mm2
Flexural Strength (28 days at 20oC): 10-13N/mm2
Bond strength (28 days at 20oC):  approx. 2N/mm2
Min. Application Temperature: +8oC.

How to use:

1. Levelling Brick or Blockwork walls 

Onto a thoroughly pre-wetted substrate, free from dust and other contaminants, apply a polymer-modified, fibre-reinforced levelling base render, in two or more applications using aluminium or stainless steel straight edges. Each wall must be finished in one working day to avoid day joints.

Our Technical Department will advise on mix design of the base creed or application details, over dissimilar materials, upon request.

2. Mixing 

Mixing of TSIRCO-POLY 107S must be carried out carefully in a clean container using a slow speed industrial electric drill using a TSIRCO mixing paddle. Add the powder to clean cold water, carefully, and mix to an even, creamy consistency.

3. Application 

TSIRCO-POLY 107S may be applied to the set (wet) levelling base render or direct to a good quality fair-faced concrete, which has been thoroughly pre-dampened. Apply using successive thin trowel applications wet on wet to build up a 3mm thickness. Depending on ambient temperature great care should be taken to avoid over wetting the surface in final ‘‘trowelling up’’, remembering the set is irreversible. Continuity of work is important to achieve a smooth court wall.

Cure: Moisture is required in order to complete hydration of the material and spraying with water may be required twice a day during the fist two days after applications. TSIRCO-POLY 107S should be allowed to fully dry before the court is used.

Lighting: As TSIRCO-POLY 107S is complete finfish it is absolutely essential that application is carried out in excellent lighting conditions to avoid trowel marks.

Coverage: TSIRCO-POLY 107S applied to a play area of 106 square meters at 3mm will require approximately 18 x 25kg bags.

Storage: Not less than 6 months stored in dry warm conditions.

Health & Safety: TSIRCO-POLY 107S is non-toxic and may be washed-off the skin with clean water. In case of ingestion or eye splashes seek medical attention.

How to Specify: All court surfaces to be finished using TSIRCO-POLY 107S in strict accordance with the recommendations of the manufacturers TSIRCON CO LTD.

PAGE  
1
Page

	Head office: 

Strovolos Industrial Zone,

P.O. Box 23863, 1687 Nicosia, CYPRUS.

Tel: +357 22 - 487029 , Fax: +357 22 - 487716

htpp://www.tsircon.com



