[image: image1.png]


TSIRCON CO LTD
MANUFACTURERS & TRADERS

OF BUILDING MATERIALS


Ημ. έκδοσης 5/2006

TSIRCO-POLY 107 FLEX

Polymeric flexible waterproofing and protective slurry

Introduction

A cement based, 2 part flexible polymeric protective and waterproofing slurry used as waterproofing coating for concrete and masonry.

Purpose

To waterproof structures such as water tanks, swimming pools, basements, balconies, roofs, e.t.c. It can also be used for rehabilitating and waterproofing existing balconies. 

Pack

25kg Solid + Liquid.

Advantages

Tsirco-poly 107 flex provides the following basic benefits:

· Flexible to bridge over cracks

· Easy to mix and apply

· Good bonding to most building materials

· Effective waterproofing

· Can be applied in a slurry consistency with stiff brush or as a trowel applied waterproofing render

· Compatibility and adhesion with sound masonry substrates (concrete, stone, brick, etc)

· Increased resistance to freezing and thawing

· Non-toxic

· Provides protection against carbonation and chloride attack

· Applied with a fibre mesh it will give extra strength and durability.

Typical Product Data
Colour: Grey

Density: Approx. 1,960kg/lt Solid & Liquid mixed
Pot Life: Approx. 30 minutes at 20(C

Elongation at break for 2mm film : > 5%
Resistance to Carbonation:



CO2 diffusion resistance RB = 480m

                    
Water vapour diffusion resistance SD = 3,0m

                   
Equivalent thickness of concrete (B 35 quality) = 120cm



Water penetration under 7 bar water pressure (DIN 1048) = 0 

Note: The spreading rate for the above results was 3kg/m2 on concrete.
Where to use

Tsirco-poly 107 flex is a flexible waterproofing slurry for concrete, concrete blocks, brick, stone and other materials.

It finds application in the following structures:

- Water reservoirs

- Tunnels

- Swimming pools

- Retaining walls

- Balconies
- e.t.c.

How to use

1.
Preparation
The surface to be treated must be clean and free from any loose particles and other contaminants such as oil, grease, dust, e.t.c. Where the substrate is steel or other metal surface, any scale, rust, oil and grease should be removed. Repair all cracks and fill any cavities using tsirco-poly 122/122l or any other material from our concrete repairs, recommended range of products, prior to the application of tsirco-poly 107 flex.

2.
Mixing
When mixing, use a clean container. Pour part a (liquid) and then add part b (solid) and mix thoroughly, preferably with a slow speed mechanical stirrer, until uniform slurry is achieved. A trowelable consistency can be achieved by modifying the ratio of Solid to Liquid. Do not use water or other solvent to thin down the mixture.

3.
Application
Dampen surface immediately before the application of tsirco-poly 107 flex. Apply material either by stiff brush or trowel. For brush application the material must be of slurry consistency. In case that a fibre mesh will be applied this should be placed between the first and second layer. After second layer application rub down the surface using a soft dry sponge to achieve a smooth finish if necessary.

4.
Coverage
1,0-2,0kg/m² per coat. Minimum two coats are recommended.
5.
Application Temperature
Minimum application temperature: 8oC.

6.
Handling Precautions
TSIRCO-POLY 107 FLEX is a non-toxic slurry. Any splashes to the eyes must be washed off immediately with clean water but if irritation persists, seek medical advice.

Storage Life

Not less than six months if kept in manufacturers’ undamaged sealed containers and stored in a dry and cool environment away from direct sunlight and frost.

How to specify

To be used strictly in accordance with the instructions of the manufacturers TSIRCON CO. LTD. 
PAGE  
1
Page

	Head office: 

Strovolos Industrial Zone,

P.O. Box 23863, 1687 Nicosia, CYPRUS.

Tel: +357 22 487029, Fax: +357 22 487716

htpp://www.tsircon.com



