[image: image1.png]


TSIRCON CO LTD
MANUFACTURERS & TRADERS

OF BUILDING MATERIALS


Ημ. έκδοσης 2/2004

TSIRCO-PU PAINT

Polyurethane protective paint for Walls and Floors

Product: A protective coating for industrial floors and walls.

Composition: Two-part polyurethane.

Purpose: A protective and decorative polyurethane coating for floors and walls that gives chemical and abrasion resistance to all kinds of Industrial floors. It can be used both internally and externally without any discolourization. It will resist most chemical and is suitable for:

◊ Parking Areas

◊ Laboratories

◊ Showrooms

◊ Industrial Floors

◊ Rendered and fair-faced walls e.t.c

Usage: 130-150gr/m2/coat.

Pack: 10kg packs.

Advantages:

Tsirco-pu paint offers the following major advantages:

· Resistance to chemicals. The coating is insoluble and unmeltable by solvents. It can resist the solvents for cleaning paints on walls and floors.

· Resistance to disinfectants and fungus.

· Dirt-pick up resistance and easy to clean.

· Good adhesion to mineral substrates.

· Weather resistance, (light stable and chalk resistant).

· Resistance to abrasion and wear.

· Good water vapour diffusion.

How to use:

1.  Preparation

Surfaces, which are to be treated with tsirco-pu paint must be structurally sound, clean and free from loose and other materials and other contaminants such as oil, grease, dust, paint or other surface coatings.

2.  Priming

If the surface to be treated is dense, such as fair-face concrete, then TSIRCO-pu primer should be applied before the application of tsirco-pu paint. Tsirco-pu primer is a two-part polyurethane, low viscosity clear coating which has high penetration. To mix the tsirco-pu primer pour component a and component b into a clean metal container and mixed well for at least 3 minutes preferably using a mechanical stirrer. Apply the material using brush, spray or roller.

3.  Mixing and Application of Coating

The mixing of tsirco-pu paint is similar to that of the primer. The material consists of two parts, component a and component b. pour the content of component B into the can containing component a and mix thoroughly by using a mechanical stirrer until the material obtains a uniform consistency.

Apply tsirco-pu paint to the prepared surface as soon as the primer is tack-free. The application is done by roller, brush or spray. 

Cleaning: All tools must be cleaned with tsirco-pu solvent immediately after use.

Handling Precautions: Handle with care to prevent skin irritation.
When dealing with polyurethane products, it is essential that operators:
a. Avoid contact with skin, eyes and clothing. In case of accidental contact with skin or eyes, thoroughly wash skin with plenty of water and seek medical advice.

b. Do not smoke.

c. Avoid naked flames or lights.

d. Avoid sparks.

e. Prevent accumulation of vapour, through ventilation of the area until product has cured.

Storage Life: Not less than 6 months if kept in manufacturers undamaged sealed containers and stored in dry and cool conditions away from direct sunlight.

PAGE  
1
Page

	Head office: 

Strovolos Industrial Zone,

P.O. Box 23863, 1687 Nicosia, CYPRUS.

Tel: +357 22 - 487029 , Fax: +357 22 - 487716

htpp://www.tsircon.com



