[image: image1.png]


TSIRCON CO LTD
MANUFACTURERS & TRADERS

OF BUILDING MATERIALS


Ημ. έκδοσης 10/2004
TSIRCO-REP 122

Early High Strength Non-shrink repair mortar

Introduction: High early strength, non-shrink thixotropic repair mortar for vertical, horizontal and overhead repairs. 

Composition: Tsirco-rep 122 is a cementitious repair mortar reinforced with fibbers. It contains special cements and additives and specially selected aggregates.

Purpose:

To be used as an economical, easy to use and effective repair mortar for concrete structures with the following advantages:

· Non-shrink.

· Rapid gain of mechanical properties (high early strength).

· High compressive, tensile and flexural strength.

· Good resistance to water, oil, chlorides and other chemicals.

· High resistance to frost.

· Resistance to abrasion.

· Very good adhesion to concrete substrate. Primer not necessary.

· Non-toxic.

Usage: 2,2kg tsirco-rep 122 will produce about 1 lt of mortar.

Pack: 25kg. 

Properties:

Colour: Grey

Density: Around 2,2kg/lt

Compressive strength at 20oC: At 24 hours > 20N/mm2
                                                  At   3 days > 35N/mm2

                                                  At 28 days > 50N/mm2
Flexural Strength:

At 28 days: > 10N/mm2
Bond Strength:

At 28 days: > 3N/mm2
Where to use:

As high early strength economical repair mortar for:

· Honeycomb surfaces on beams, columns, slabs, walls, e.t.c.

· Bridges.

· Parking aprons.

· Runways.

· Water retaining structures.

· Factory floors.

· Any kind of concrete structures.

How to use:

1.  Preparation

The surfaces to be treated must be clean and free from loose material and other contaminants such as oil, grease, dust, e.t.c. When patching on to steel or other metal surfaces any scale, rust, oil and grease should be removed. When patching on traffic areas like parking places and garages, acid etching and/or sandblasting should be preceded to ensure that no grease or tyre marks will be present. Cleaning can also be done by any other mechanical means.

2.  Mixing

Add the material in water and stir thoroughly using preferably a mechanical mixer for about two minutes. Leave the material to stand for another two minutes and stir again.

Mixing Ration: 25kg tsirco-rep 122 with about 3,5-3,7 lt of water.

3.  Application

Saturate the substrate sufficiently with water prior to the application of tsiRco-rep 122. While the substrate is still damp place the mortar using trowel or putty. Make sure that the cavities are thoroughly filled and compacted. For very porous or week substrates prime the surface with tsiRco-poly 101, in order to improve the substrate before applying tsirco-rep 122.
Application Temperature:

Minimum working temperature: +8oC.

Application Thickness:

Minimum: 2mm

Maximum: 30mm

For thickness over 30mm add clean, moist, coarse sand or alternatively work in layers.

Cleaning: Use plain water to clean all equipment immediately after their use.

Curing: Use any approved curing method.

Storage Life: Not less than 6 months provided the product is kept in the manufacturers sealed containers and stored in a dry and cool environment away from frost and dampness.

Handling Precautions: TSIRCO-REP 122 is non-toxic. Use gloves if required to apply by hand. In case of eye splashes wash thoroughly with plenty of water, but if irritation persists seek medical advice.

PAGE  
1
Page

	Head office: 

Strovolos Industrial Zone,

P.O. Box 23863, 1687 Nicosia, CYPRUS.

Tel: +357 22 - 487029 , Fax: +357 22 - 487716

htpp://www.tsircon.com



