[image: image1.png]


TSIRCON CO LTD
MANUFACTURERS & TRADERS

OF BUILDING MATERIALS


Ημ. έκδοσης 6/2006
TSIRCO-RES 601
Lightweight Epoxy Mortar used for vertical and overhead surfaces
Product

A three component lightweight Epoxy Mortar for concrete repairs.
Composition

Epoxy Resins (Base and Hardener) and lightweight Aggregates.
Purpose

For restoration and repairs of concrete surfaces
Density 
1,7kg/lt (at 20ºC)
Pack

4 and 8 kg
Where to use
TSIRCO -RES 601 can be used on all kinds of surfaces, especially on soffit work due to its lightness. It can be used in very thin (2-3mm) and thick (2-3cm) layers for structural repairs of columns, walls, soffits, floors, etc. It is also used as a bedding material for tiles and for the lining of concrete tanks.
HOW TO USE
1.
Preparation
The substrate, where the material is to be applied, must be free from dust, oil, paints or any other contaminants.
2.
Priming
We recommend the use of TSIRCO-RES 101 as a primer prior to the application of TSIRCO-RES 601. 
3.
Mixing
TSIRCO-RES 601 consists of the Base, the Hardener and fine Aggregates: 

Pour the Hardener into the Base and mix thoroughly, preferably with a slow speed mechanical mixer. After placing the mixed material into a backet, continue mixing with the gradual addition of the lightweight Aggregates, until the mix comes to a constant consistency.
4.
Application
After mixing and priming, apply TSIRCO-RES 601 while the primer is still tacky, with a wood floater, steel trowel or by hand (wearing protective gloves), ensuring good compaction. In order to achieve a smooth surface wipe the trowel with a cloth dampened with TSIRCO-EPOSOLVE.
5.
Cleaning
All tools can be cleaned with TSIRCO-EPOSOLVE immediately after use.

6.
Handling Precautions
During mixing and application, the operators must ware gloves and goggles. Always handle resins with care to prevent skin irritation. For detailed recommendations you may consult the “TSIRCO- RES Handling Guide”.
Storage Life

Not less than one year if kept in manufactures’ undamaged sealed containers and stored in dry and cool conditions away from direct sunlight and frost.
How to specify

Use TSIRCO-RES 601 strictly in accordance with the instructions of the manufacturers, TSIRCON CO. LTD.

PAGE  
1
Page

	Head office: 

Strovolos Industrial Zone,

P.O. Box 23863, 1687 Nicosia, CYPRUS.

Tel: +357 22 487029, Fax: +357 22 487716

htpp://www.tsircon.com



