[image: image1.png]


TSIRCON CO LTD
MANUFACTURERS & TRADERS

OF BUILDING MATERIALS


Ημ. έκδοσης 5/2004

TSIRCO-SL COMPOUND

Polymeric self-levelling cement based compound

Product: Economic Self Levelling Polymeric compound which is easy to apply with good resistance to chemical attack and abrasion. 

Composition: A cement mix incorporating special cements, fillers and other additives to produce, when mixed with water, a self-levelling compound for industrial floors.

Purpose: For construction of new, or upgrading existing  industrial floors (e.g. concrete roads, parkings, warehouses, factories, show rooms, etc).

How to use:

1. Preparation 

The surface before application must be clean from loose or friable particles and free from dust, oil and any other contaminous. The cleaning operation can be achieved by gridblasting, water jetting, acid etching, grinding or any other appropriate method.

2. Mixing
For mixing, use a clean bucket. Mix the Tsirco-SL Compound with clean water at a ratio 4:1 respectively. It is preferable for the mixing to be done by a slow speed mechanical mixer until a uniform and homogeneous mix is achieved.

3. Application
After watering the surface pore the material and spread it over the surface with a trowel or ‘squeegee’ to the required thickness. If the surface is porous then you should use Tsirco-Res 481 as a primer. If chemical resistance or increased wearing resistance is required it is recommended to apply any of our range of epoxy toppings or coatings such as Tsirco-Res 408, Tsirco-Res SL e.t.c over Tsirco-SL Compound.

Coverage: Approximately 1.9kg/m²/mm thickness. 

Cleaning: Right after use, clean the equipment with water.

Workability Time: 20 minutes at 20oC.

Setting Time: 120 minutes at 20oC.

Storage: Store at a dry environment and away from direct sunlight.

Protective Measures: The material is non-harmful but avoid contact with the skin and use gloves.

PAGE  
1
Page

	Head office: 

Strovolos Industrial Zone,

P.O. Box 23863, 1687 Nicosia, CYPRUS.

Tel: +357 22 - 487029 , Fax: +357 22 - 487716

htpp://www.tsircon.com



