[image: image1.png]


TSIRCON CO LTD
MANUFACTURERS & TRADERS

OF BUILDING MATERIALS


Ημ. έκδοσης 12/2003

TSIRCO-ANTIGRAFFITI

Protective and antigraffitic paint

Product: A protective coating with antigraffiti properties.

Composition: Two-part polyurethane.

Purpose: To protect concrete and other mineral surfaces such as rendered surfaces, fibre-reinforced plaster-boards, e.t.c., from the chemicals present in the atmosphere or from vandalism,  giving also antigraffitic properties.

Usage: 130-150gr/m2/coat.

Pack: 10kg packs.

Advantages:

Tsirco-antigraffiti coating offers the following major advantages:

· Resistance to chemicals. The coating is insoluble and unmeltable by solvents. It can resist the solvents for cleaning paints on walls.

· Resistance to disinfectants and fungus.

· Dirt-pick up resistance and easy to clean.

· Good adhesion to mineral substrates.

· Weather resistance, (light stable and chalk resistant).

· Resistance to abrasion and wear.

· Good water vapour diffusion.

Where to use: Tsirco-antigraffiti being resistant to solvents used in cleaning graffiti from walls, it is the ideal coating for public buildings such as schools, stadiums, bridges, hospitals, clubs, or even private house buildings.

How to use:

1.  Preparation

Surfaces, which are to be treated with tsirco-ANTIGRAFFITI must be structurally sound, clean and free from loose and other materials and other contaminants such as oil, grease, dust, paint or other surface coatings.

2.  Priming

If the surface to be treated is dense, such as fair-face concrete, then TSIRCO-antigraffiti primer should be applied before the application of tsirco-antigraffiti. Tsirco-antigraffiti primer is a two-part polyurethane, low viscosity clear coating which has high penetration. To mix the tsirco-antigraffiti primer pour component a and component b into a clean metal container and mixed well for at least 3 minutes preferably using a mechanical stirrer. Apply the material using brush, spray or roller.

3.  Mixing and Application of Coating

The mixing of tsirco-antigraffiti coating is similar to that of the primer. The material consists of two parts, component a and component b. pour the content of component B into the can containing component a and mix thoroughly by using a mechanical stirrer until the material obtains a uniform consistency.

Apply tsirco-antigraffiti coating to the prepared surface as soon as the primer is tack-free. The application is done by roller, brush or spray. In the case that the application is done by the spray method, dilute the mixed product with up to 5% tsirco-antigraffiti dilute.

Cleaning: All tools must be cleaned with tsirco-pu solvent immediately after use.

Handling Precautions: Handle with care to prevent skin irritation.

When dealing with polyurethane products it is essential that operators:
a. Avoid contact with skin, eyes and clothing. In case of accidental contact with skin or eyes, thoroughly wash skin with plenty of water and seek medical advice.

b. Do not smoke.

c. Avoid naked flames or lights.

d. Avoid sparks.

e. Prevent accumulation of vapour, through ventilation of the area until product has cured.

Storage Life: Not less than 6 months if kept in manufacturers undamaged sealed containers and stored in dry and cool conditions away from direct sunlight.

PAGE  
1
Page

	Head office: 

Strovolos Industrial Zone,

P.O. Box 23863, 1687 Nicosia, CYPRUS.

Tel: +357 22 - 487029 , Fax: +357 22 - 487716

htpp://www.tsircon.com



