[image: image1.png]


TSIRCON CO LTD
MANUFACTURERS & TRADERS

OF BUILDING MATERIALS


Ημ. έκδοσης 12/2003

Z Joint Profile

[image: image2.png]


Crack Inducer

Description: An easily applied preformed PVC profile that induces controlled cracking in continuously laid concrete or screed specially suitable for heavy traffic applications. It is specially design to transfer the load from one bay on to the next with the moving load. 

Advantages:

· Enables increased production. The concrete can be laid in the whole area in the same day.

· No need for costly cutting and filling of joints. It creates an excellent key to concrete.

· Excellent anchoring in concrete due to the “key” section.

· Retains unchanged its shape and dimensions. It can also be used as a guidance for the leveling of concrete or screed.

· It can also be used in concrete floors subject to heavy traffic loads.

Technical Characteristics:

	Material
	: Polyvinyl chloride compound, hard

	Density
	: 1,40g/ml

	Yield Strength
	: 46N/mm²
	(BS2782:Part II:Method 1110)

	% of Elongation
	: 40% 
	

	Modulus of Elasticity
	: 2000N/mm²

	Vicat Softening Temperature
	: 82°C
	(BS2782:Part I:Method 120B)


�








PAGE  
	Head office: 

Strovolos Industrial Zone,

P.O. Box 23863, 1687 Nicosia, CYPRUS.

Tel: +357 22 - 487029 , Fax: +357 22 - 487716

htpp://www.tsircon.com



